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13 Knight Street, Spalding PE11 3RA – Grade II Listed

Specifcation of Repair Works to Boundary Wall
Restoration and rebuilding works to listed brick boundary wall.

Phase 1

Take down 15 linear metres of existing damaged wall.

The removal will allow for a splayed edge to allow the new wall to tie strongly into the old wall.

All bricks will be cleaned and sorted for re-use where possible

All damaged bricks will be discarded and removed from site

Phase 2

Construct new brick wall to the same style as existing wall.

Build new piers in original positions at the back of the wall to help with stability.

Create new dentil feature and rake to coping as per existing wall

All mortar will be hydraulic lime 3.5 NHL at a mix ratio of 3-1.

Please note that we may upgrade the lime to NHL 5 if the weather is particularly cold, This will add further protection from frost.

Sand will be Heritage sand mixture with aggregates 3mm to nominal.

All mortar will be brushed back flush to reveal brickwork arris and stone aggregate within the mortar mix.

Fully protect the lime mix from frost with frost protection.

Please note this may need to be kept in place after the contract has finished  to protect from frost damage whist the lime slowly cures.

Matching bricks have been sourced from Brocklebank Reclaims in Louth and will be used where required.
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